## Slide 1
OptoFab Node
Michael Withford
(Node Director)
Specialty fibre fabrication (mPOF)
Tapering, characterisation
Simon Fleming
Richard Lwin
Alex Arygos
Eric Magi
Dave O’Connor
Cleanroom facilities
Photomask fabrication
Ben Johnston
Rob Williams
Marty Ams (makes it look pretty  )
Specialty Fibres, Biosensors, glass chemistry
Tanya Monro
Heike Ependorff-Heidepriem
Luis Lima-Marques
Notes: 1

## Slide 2
Synergies within the OptoFab node. e.g. ZBLAN waveguide laser
Benefits of NCRIS and EIF schemes
Laser micromachining at Macquarie, existing and new facilities
Some successful projects
  MNRL at Monash
  Melbourne University diamond devices
  Ge nano-electronics at UNSW
- Recent benefactors at USyd and MQ
Overview

## Slide 3
Node Synergies…
Future Vision: Providing a start to finish approach to glass and polymer photonics
Materials…
Fibre design and Fab…
3D and planar
fabrication…
Modification and
characterisation..
Assembly and
packaging..

## Slide 4
Internal example
ZBLAN waveguide laser
S. Gross1, D. Lancaster2, H. Ebendorff-Heidepriem2, K. Kuan2, T.M. Monro2, M. J. Withford1, and A. Fuerbach1
1Centre for Ultrahigh bandwidth Devices for Optical Systems (CUDOS),
MQ Photonics Research Centre, Department of Physics and Astronomy, Macquarie University, NSW 2109, Australia
2Institute for Photonics and Advanced Sensing (IPAS)
School of Chemistry and Physics, The University of Adelaide, SA, 5005, Australia
Input coupler mirror
Output coupler mirror
9 mm Tm:ZBLAN sample
Silicon filter
0.1 NA 25 µm core fibre
Collimation and launch optics
HR @ 2000 nm
HT @ 790 nm
OC @ 2000 nm
790 nm pump light
f = 20 mm
f = 20 mm
1880 nm output
50 µm
Top surface

## Slide 5
Goal: to make this type of interaction with OptoFab happen for a wide range of users. (And in the long term $elf $ustaining)
Ingot of Tm3+ doped ZBLAN, fabricated from melt at University of Adelaide.
Femtosecond laser inscription of waveguides and characterisation at Macquarie
Laser assembly and characterisation at Adelaide

## Slide 6: Track Record
Solid growth
Large external user base
  2009-10 reporting period = 64%
Track record industry / PFRA interaction
  2009-10 reporting period = 17%
User satisfaction - high
OptoFab

## Slide 7: Benefits due to NCRIS & EIF support
NCRIS Investment:
Optofab established on existing facilities
  Infrastructure ranging from low to high tech
  Predominantly customised systems
EIF Investment:
Build new, transformational facilities
  Many customised systems
  Increased emphasis on integration
  Large scale wafer, optical lithography
OptoFab

## Slide 8: Benefits due to NCRIS & EIF support (cont.)
NCRIS Investment:
Major benefits
  facilitate access to established, mature expertise
  ensure continuity of expertise
  support facility operating / maintenance costs
EIF Investment:
Major benefits:
  Enable open access to emerging expertise
  Fast track development of emerging expertise
    personnel + equipment
OptoFab

## Slide 9: New Home for Optofab
Australian Institute for Nanoscience
- University of Sydney
10,500 m2 building
  $110M, EIF Super Science $40M
  Ready for occupancy 2013 – 2014
Purpose-built Nanofabrication Facility – 1200 m2 clean room
Photonics - prime reason for this facility
  Co-locate with quantum science
Bandwidth Foundry, with i-line stepper and DWL, to re-locate
9
Institute for Photonics & Advanced Sensing (IPAS) Building, University of Adelaide
$95M purpose-built building, HEEF, Uni & State Government support
  Ready for occupancy 2013
50% of the building dedicated to research facilities for optical materials science, optical fibre fabrication, laser development, surface science and sensor research
Laboratories that bring together biological and photonics capabilities
Australian Hearing Hub
- Macquarie University
Approx 20,000 m2 building
  $140M, HEEF and Uni
  Ready for occupancy late 2012
Purpose-built Fabrication Facility
  >200 m2 low vibration (VC-E)
  >100 m2 office space
Relocate laser micromachining facilities, sample preparation and characterisation
Co-located with Cochlear (R&D), Aust. Hearing Associations, and non-for-profit organisations
Artist impression (USyd)
Artist impression (UAdel)
Artist impression (Macq)

## Slide 10
Laser Micromachining
Notes: 10

## Slide 11
MQ Facilities
Exisiting facilities supported by NCRIS from 2008
- Nano-second Vis-UV laser machining facility (JDSU Q-series 532nm)
- Limited time on the Hurricane Femtosecond system
- Aerotech ATS-100 stages and controller
- Aerotech Fibre align stages with 30cm air-bearing stage and controller

## Slide 12
MQ Facilities (Coming soon)
New facilities Funded by EIF from 2010
RegA Femtosecond Laser Facility
Diamond MOCVD and nanoassembly facility
Optical characterisation suite

## Slide 13
Some projects…

## Slide 14
MNRL at Monash
Prof. James Friend
Dr. Leslie Yeo
$7mill in funding with projects in microfluidics, acoustics, piezoelectrics, micromechanical systems, drug delivery….
Good match with our capabilities
Great people to work for;
patient, happy to work through several iterations of a part
Generous with cross promotion
Publish often and with acknowledgments
Attract good press
Now heavily involved with ANFF in Melbourne and understand the deal.

## Slide 15
Laser Micromachining Solutions (MQ)
Testimonial: A/Prof James Friend – Monash University, Aug 2009
  “When we started this work, we chose XXXXXXX, a popular laser machining job shop in the US in theory capable of addressing our needs. The results were—politely stated—abysmal. After learning of A/Prof Withford’s facility, we tried their services and the result has been.....:”
  2 Provisional Patents
  4 journal papers
  2 successful grant application + 2 more pending.

## Slide 16
MNRL at Monash
Principle:
Piezo driven mechanical resonance for producing good torque and RPMs in a machine of the order of 1mm3
Progess:
~130 RPS
7800RPM
Brett Watson, Leslie Yeo, and James Friend, A study on axial and torsional resonant mode matching for a mechanical
system with complex nonlinear geometries, REVIEW OF SCIENTIFIC INSTRUMENTS 81, 063901 2010
Concept:
http://www.youtube.com/watch?v=VRMEtCCDR_E

## Slide 17
What we make…
- Start with 32G (230um) hypodermic tube
- Stages in a lathe configuration - 10-50mW of 266nm ns pulses, 500Hz.

## Slide 18
Turn and burn…
- 0.5mm long
11 turns/mm
Two tracks (180deg)
Cuts ~80% of the way through sidewall for best resonance performance
Lots of iterations to get it right
http://www.youtube.com/user/MNRLMonash?blend=2&ob=1#p/u/11/XYdlA4Pv9Rg Earlier model with a few RPM
Other bits:
Rotor for measuring the RPM, cut from 25um copper
Propeller tails to make it swim (coming soon)

## Slide 19
Variations…
- Slotted stator for 3 axis articulation
Blade type propellers (300um span)

## Slide 20
Diamond at Melbourne University
Diamond electrode array sectioning
Plumbing ports for Diamond microfluidics

## Slide 21
Another successful user…

## Slide 22
Ge nanoelectronics at UNSW CQCT
G Scappucci, G Capellini, B. Johnston, W. M. Klesse, J. A. Miwa, and M Y Simmons.
A complete fabrication route for atomic-scale, donor-based devices in single-crystal germanium. Submitted to Nanoletters.
Abstract: Despite the rapidly growing interest in Ge for ultra-scaled classical transistors and innovative quantum devices, the field of Ge nanoelectronics is still in its infancy. One major hurdle has been electron confinement since fast dopant diffusion occurs when traditional Si CMOS fabrication processes are applied to Ge. We demonstrate a complete fabrication route for atomic-scale, donor-based devices in single-crystal Ge using a combination of scanning tunnelling microscope (STM) lithography and high quality crystal growth. The cornerstone of this fabrication process is an innovative lithographic procedure based on direct laser patterning of the semiconductor surface, allowing the gap between atomic-scale STM-patterned structures and the outside world to be bridged…..

## Slide 23
Some recent benefactors at USyd
Cenk: - Multilayered Steel-Au-Steel discs for shear force compliance tests
Maryanne, Anna et.al.: - Patterning of metal coated PMMA arrays, THz meta material
Pourandokht: sub-10um pinholes

## Slide 24
Some recent benefactors at MQ
Josh Brown and Chris McMahon
- Moly parts for the nitride growth and synchrontron runs
- Masks for lithography and evaporation
Carlo and Torsten
50um grids for locating the AFM
Martin and Sandeep
Numbered grids on coverslides for observing the growth of stem cells from day to day

## Slide 25
Providing nano and micro-fabrication facilities for Australia’s researchers
www.anff.org.au

## Slide 26
Thanks